CERTIFICATION REPORT

Certification of Charpy V-notch reference test pieces of 150 J nominal absorbed energy

##### Certified Reference Materials ERM®-FA415k,

##### ERM®-FA415l, ERM®-FA415m, ERM®-FA415n,

##### ERM®-FA415o

The mission of IRMM is to promote a common and reliable European measurement system in support of EU policies.

European Commission

Directorate-General Joint Research Centre

Institute for Reference Materials and Measurements

Contact information

CRM Sales

European Commission

Directorate-General Joint Research Centre

Institute for Reference Materials and Measurements

Retieseweg 111

B-2440 Geel • Belgium

Email: jrc-irmm-rm-sales@ec.europa.eu

Tel.: +32 (0)14 571 705

Fax: +32 (0)14 590 406

http://www.irmm.jrc.be

http://www.jrc.ec.europa.eu

http://www.erm-crm.org

Legal Notice

Neither the European Commission nor any person acting on behalf of the Commission is responsible for the use which might be made of the following information.

EUR Report 22699 EN

ISSN 1018-5593

ISBN 978-92-79-05220-0

Luxembourg: Office for Official Publications of the European Communities

© European Communities, 2007

Reproduction is authorised provided the source is acknowledged

Printed in Belgium

CERTIFICATION REPORT

Certification of Charpy V-notch reference test pieces of 150 J nominal absorbed energy

##### Certified Reference Materials ERM®-FA415k,

##### ERM®-FA415l, ERM®-FA415m, ERM®-FA415n,

##### ERM®-FA415o

G. Roebben, A. Lamberty

European Commission, Joint Research Centre

Institute for Reference Materials and Measurements (IRMM)

Geel, Belgium

European Commission

EUR 22699 EN – DG Joint Research Centre, Institute for Reference Materials and Measurements –

Certification of

Authors :G. Roebben, A. Lamberty

Luxembourg: Office for Official Publications of the European Communities

2007 – 33 pp. – 21.0 x 29.7 cm

EUR - Scientific and Technical Research series; ISSN 1018-5593

ISBN 978-92-79-05220-0

Abstract

This certification report describes the processing and characterisation of ERM®-FA415k, ERM®-FA415l, ERM®-FA415m, ERM®-FA415n, and ERM®-FA415o, five batches of Charpy V-notch certified reference test pieces. Sets of five of these test pieces are used for the verification of pendulum impact test machines according to EN 10045-2 (Charpy impact test on metallic materials, Part 2. Method for the verification of impact testing machines [1]) or according to ISO 148-2 (Metallic materials - Charpy pendulum impact test – Part 2: Verification of test machines [2]). The certified value for KV (= energy required to break a V-notched test piece using a pendulum impact test machine) and the associated uncertainty (k = 2 corresponding to a confidence level of 95 %) calculated for the mean of a set of five test pieces, are:

| Batch-code | Certified KV-value | Expanded uncertainty (k=2, 95 % confidence level) |
| --- | --- | --- |
| ERM®-FA415k | 149.0 | 4.4 |
| ERM®-FA415l | 147.2 | 3.8 |
| ERM®-FA415m | 149.0 | 4.3 |
| ERM®-FA415n | 149.3 | 3.8 |
| ERM®-FA415o | 149.9 | 4.2 |

The certified values are traceable to the Charpy impact test method as described in EN 10045-1 [3] and ISO 148 [4], via the corresponding Master Batch ERM®-FA415b of the same nominal absorbed energy (150 J).

ERM®-FA415k, ERM®-FA415l, ERM®-FA415m, ERM®-FA415n, and ERM®-FA415o have been accepted as European Reference Material® (ERM®) after successful peer evaluation by the partners of the European Reference Materials consortium.

| The mission of the Joint Research Centre is to provide customer-driven scientific and technical support for the conception, development, implementation and monitoring of European Union policies. As a service of the European Commission, the JRC functions as a reference centre of science and technology for the Community. Close to the policy-making process, it serves the common interest of the Member States, while being independent of special interests, whether private or national. |  | 15 LA-NA-22699-EN-C |
| --- | --- | --- |